SECTION 12 34 00

LAMINATE CLAD CASEWORK

# PART 1 – PRODUCTS

1.01	ACCEPTABLE MANUFACTURERS:

- Manufacturer:

  - TMI Systems Corporation.

    - Drawings and specifications are based on manufacturer’s literature from TMI SYSTEMS CORPORATION, 50 South Third Avenue West, Dickinson, North Dakota, 58601, Phone: 800-456-6716, fixed modular, flexible rail mounted, and mobile casework and accessories.

    - Other manufacturers shall comply with the minimum levels of material and detailing indicated on the drawings or as specified.

1.02	MATERIALS:

  - Edging Materials:

- 1mm PVC banding, machine applied.

- 3mm PVC banding, machine applied and machine profiled to 1/8 inch radius.

1.03	FABRICATION:

A.	Cabinet Body Construction

1.	Exposed and semi-exposed edges: 1mm PVC banding, machine applied.

2.	Adjustable Shelves in Cabinet

a.	Core:  Particleboard

b.	Thickness:  3/4 inch up to 30 inches wide, 1 inch over 30 inches wide.

c.	Banding:  1mm PVC machine applied, front edge only.

B.	Door/Drawer Fronts

1.	Core:  Particleboard

2.	Finish:  High-pressure decorative VGS laminate (0.028”) exterior, balanced with high-pressure cabinet liner CLS (0.020”) interior.  Use of TFM on exterior or interior surfaces of door/drawer fronts will not be permitted.

3.	Banding:  3mm PVC machine applied, with external edges and outside corners machine profiled to 1/8 inch radius.

1.04	DECORATIVE LAMINATE COUNTERTOPS:

- Core:

- All countertops except at sink elevations: 1-1/8 inch thick ANSI A208.1-1993 M-2 particleboard.

- Countertops at sink elevations: 1-1/8 inch thick ANSI A208.1-1993 M-3 moisture resistant (MR) particleboard.

  - Surface:  High-pressure decorative HGS/HGP (0.042” – 0.048”) laminate with balanced backer sheeting.

  - Edges, including applied backsplash:  3mm PVC machine applied, with exposed edges and corners machine profiled to 1/8 inch radius.

- All countertops joints must be dry fit at the factory to check for consistency in color from one panel to the other and overall finished panel thickness, resulting in a high quality product easy to install.

1.03 	COLOR SELECTION:

    - PVC Banding Color Selection:

- 3mm PVC: Select from the TMI Vendor Stock PVC Program or similar.  Program offering must include over 180 pattern, woodgrain and solid colors matched to Wilsonart®, Formica®, Nevamar® and Pionite® laminates.

- 1mm PVC: Select from the TMI Vendor Stock PVC Program or similar.  Program offering must include over 180 pattern, woodgrain and solid colors matched to Wilsonart®, Formica®, Nevamar® and Pionite® laminates.