SECTION 123400 or SECTION 064023

LAMINATED WALL PANELS & HARDWARE

(Merge into TMI Laminate Clad Casework Specifications.)

1.01	MATERIALS

- Core Materials – Laminated Wall Panels:

CHOOSE ONE:

  - Particleboard:  3/4 inch thickness.  Industrial Grade average 45-pound density particleboard, ANSI A 208.1-2009, M-2 requirements.

- MDF:  Medium Density Fiberboard. 3/4 inch thickness. Industrial grade average 48-pound density MDF produced, from 100% post-industrial recycled wood fiber, manufactured with a formaldehyde free adhesive system which meets the requirements of ANSI A208.2, Grade 150.

- CFC Combo Plywood Core:  3/4 inch thickness (7-ply). Veneer core consisting of Western softwood inner core, with outer plys on both faces consisting of medium density fiberboard (MDF) resulting in a smooth laminating surface with minimal telegraphing. Roseburg SkyPly CFC Veneer Core panels or approved equal with no added urea-formaldehyde.

- Reveal Panels - Medium Density Fiberboard 1/4 inch or 5/32 inch thickness:  Minimum average density 45-50 lbs., ANSI A208.2-2009 requirements.

- Decorative Laminates:

- Wall Panels: High-pressure decorative laminate VGS (.028), meeting ISO 4586 testing. GREENGUARD Indoor Air Quality Certified.

CHOOSE ONE:

- Reveal Panels: Thermally fused (TFL) laminate, meeting ISO 4586 Testing.

- Reveal Panels: High-pressure decorative laminate VGS (.028), meeting ISO 4586 testing. GREENGUARD Indoor Air Quality Certified.

- Edging Materials:

- 1mm PVC banding, machine applied and trimmed.

1.02	SPECIALTY ITEMS

    - Laminated Wall Panels:

- Fabricate panels to dimensions, profiles, and details shown. Fabricate panels to achieve specified reveal dimensions shown on drawings.

- All panel components must go through a supplemental sizing process after cutting, producing a panel precisely finished in size and square to within 0.010 inches, ensuring strict dimensional quality and structural integrity in the final fabricated panels.

- Wall panels finished with VGS laminate on exposed surface, balance with CLS (.024) or VGS (.028) laminate on the back side. Balanced construction of all 3/4 inch thick laminated panels is mandatory. Unfinished core stock surfaces, even on concealed surfaces will not be permitted.

- All four edges of each individual wall panel finished with specified 1mm PVC edgebanding, machine applied and trimmed. Match laminate selection when available.

- Reveal panels of 1/4 inch or 5/32 inch MDF to be finished with specified laminate, cut into 3 inch x 95 inch strips by the manufacturer. Cut to length in the field as needed for installation.

- Hardware: Extruded Z-clips of treated hardened aluminum alloy (6005-T6) tempered in accordance with ASTM B221, with grooved back and 3/8 inch lift-off.  Z-clip hardware to be provided by panel manufacturer, attached in the field to each individual panel and walls utilizing No. 8 wood screws, with maximum vertical spacing of Z-clips not exceeding 27 inches.  Hardware to remain concealed after installation is completed.

1.03 	COLOR SELECTION:

    - Laminated Wall Panels Color Selection:

- Select from the full range of standard non-premium Wilsonart® and Formica® stock color charts.

- Thermally fused (TFL) laminate matched to Black color.

    - PVC Edgebanding Color Selection:

- Laminated Wall Panels: Select from the TMI Vendor Stock PVC Program, including over 180 pattern, woodgrain and solid colors matched to Wilsonart® and Formica® laminates.